Chemical & Metallurgical Consultants 
(972) 272-7337 FAX (972) 272-7790 
Universal Laboratory, Inc. 

1726 Commerce St Garland, Texas 75040-6710 
DATE: 
4-15-99 
TEST NO.: 26342 
Page 1 of 1 
FOR: 
FLAME SAFE WOOD PRODUCTS, INC. 2653 WARFIELD AVE. 
FORT WORTH, TX 76106 
Plant Contact: Louis Jacobini 
Background: 	Flame Safe Wood Products submitted Spruce Pine Fir samples for Flame Spread Test Per ASTM E 84,1991a. Delivered to ULI in Good Condition. All testing and sample preparation performed by Universal personnel with no outside services required. 
The following information is provided: Order Entry Log Date: 4-12-99 Log # 459161 
Product Identification: Vacuum Pressure Fire Retarded Treated Wood 
3 Panels 24" x 96" Spruce Pine Fir, fabricated with 2" x 4" No.2 SPF 
Test Results: 	Material: 	Spruce Pine Fir 
	Thickness: 	2" 
Calibration Media Red Oak/Cement Board 
	Moisture: 	5% 
	Draft Inches: 	.15 
	Leakage Test: 	Acceptable 
Air Velocity Average Ft/Min.: 150 
	G~: 	Natural 
	Preheat Temperature: 	560°F 
	Flame Spread Factor: 	(FSI - 9.6) 
	Smoke Generation (SDI): 	518.5 
Observation: Ignition Time: 
Time to Max: 
Max Temperature: 
Charing: 
Dripping: 
80 Seconds. 24.3 Minutes 681°F Moderate None 
Note: "We certify that all portions of each test performed were under continuous, direct supervision of this laboratory." 
Charles'Siamey,Director
for Universal Laboratory, Inc.