R E S E A R C H

S O U T H W E S T

INSTITUTE

6220 CULEBRA, ROA\D· P08T OFFICE DRA\WER :28510 • SAN ANTONIO, TEXAS, USA 78228-0610 • (512) 684-5111 • TELEX 2440846

CHEMISTRY AND CHEMICAL ENGlNEERING DIVISION DEPARTMENT OF FIRE TECHNOLOGY FAX (512) 522-3377

December 5, 1991

Flame Safe

2653 Warfield Avenue

Fort Worth, Texas 76106

Attn: Mr. Louis Jacobini

Re: SwRI Proje~t No. 01-4510-117-b 	FINAL REPORT

“Ignition Resistance of Aircraft Interior Materials

(FAR 25.853b 12-Second Vertical)” '

Gentlemen:

This letter constitutes our final report on your blue denim fabric with fir~ retardants~ identified as lOO-percent cotton fabric sprayed with Fabric Safe flame retardant at 400 sq.ft/gallon, submitted for evaluation by t referenced test method. The samples were prepared by the Client and received at SwRI ready for testing.

The results apply specifically to the specimens tested, in the manner tested, and not to the entire production of these or similar materials, nor to the performance when used in combination with other materials. All test data are on file and are available for review by authorized persons.

TEST METHOD AND PROCEDURE

The material Was tested in accordance with FAR 25.853b 12-Second Vertical. The test establishes a£terflame time and char length on each specimen as applicable.

The specimens were conditioned in accordance with the standard. Each specimen tested was exposed to the test flame within 15 minutes after removal from the standard atmosphere. Each specimen vas inserted into the cabinet and the 1-1/2-1n. (38.1-mm) Bunsen burner flame (approximately 1650°F) was applied vertically at the middle of the lower edge of the specimen for 12 Seconds.

The afterflame time of the specimen was recorded to the nearest

0.1 seconds and the char length to the nearest 0.1 in. (2.5 mm). The test criteria for this test are as follows:

Char Length:

Afterflame Drip Burn:

Maximum average, 8 in. Maximum average, 15 seconds Maximum average, 5 seconds

----------------------

Thl, r">Xl'1ln 10< tho inlormal>on 01.", c1i<>nl. tt m.y b9 UGOO In /1< qnl;ro'Y ~,r IhO pV'j}OO8 or :k'<:urinO pro<h>cl aCC{jpL'"",-, Irom duly lXJ<'I;.~\tvt:x:llJ.PfI(OY81 tl.LJ1hOfttB'b. Ne~h .• r thl& rf>P')(t nor tr,n nomt) 0' tho In.tlHllo ~hall 00 ~8d In pl,.lOl-eity VI t.ldv.wHSir'{J.

SAN ANTONIO. TEXAS

HOUSTON, TEXAS 	• 	OE:TROIT, r.1ICHll'M'; 	•

WASH'IINGTON, DC

Flame Safe

SwRI Project No. Ol-4510-117-b December 5, 1991

Page 2

FAR 25.853b Test Method

TRST SPECIMEN AND NUMBER OF DETERMINATIONS

The specimens were identified as 100-percent Cotton fabric with Fabric Safe flame retardant sprayed at 400 sq.ft/gallon. They were described as blue denim fabric with fire retardants. The samples were prepared by the Client and received at SwRI ready for testing. Each specimen was 2.5 x 13 in. (63.5 x 330.2 mm)t nominal thickness 6.24 in. (6.1 mm). A minimum of three specimens were tested in each the machine direction (warp) and the acrossmachine directions (filling).

TEST RESULTS

The test was conducted November 26, 1991, with the following results:

Machine Direction:

|  |  | Run 1 | Run 2 | Run 3 | Average |
| --- | --- | --- | --- | --- | --- |
| Char Length , | in. | 4.00 | 4.25 | 3.63 | 3.96 |
| After-flame 7 | sec. | 0 | 0 | 0 | 0 |
| Drip Burn, sec. |  | None | None | None | None |

ACROSS MACHINE DIRECTION:

Run 1

Run 2

Run 3

Average

Char Length, in. Afterflame, sec. Drip Burn, sec;

3.75 o None

3.63

o None

3.38

o None

3.59

o

None

The material , when tested in accordance with FAR 25.853b 12-Second Vertical test, is considered to have passed.

If you should have any questions/comments or if we can be of further assistance, please contact us.

Sincerely,

Approved by:

~;I(PJ ,~~

Alex B. Wenzel Director

Department of Fire Technology

~~~ \(l, Q.;\\ \ QM .

Gladys M Finley

Project Leader

Fire Testing Services

GMF/rr